Table 2. Magnesium reversibility as a common readout for distinguishing transfer pathways.

| Transfer contribution and representative chemistry | Reported Mg CE (%) | Reported performance context | Matched mechanistic test | Refs. |
| --- | --- | --- | --- | --- |
| Precursor availability Mg(TFSI)₂ / DME–G2–BTFE–TEP | 95.2 | Reversibility in a weakly paired formulation | Relate carrier population to Mg current; match transport and surface history. | [24] via [86] |
| Ligand rearrangement Mg(TFSI)₂ / DME–MOPA-1 | 99.5 | Reversibility with redesigned donor coordination | Compare ligand exchange and Mg current on equally conditioned surfaces. | [76] via [86] |
| Reduction selectivity Ion-paired amine electrolyte | 99.6 | Mg charge recovery over an 800-cycle readout | Quantify H₂ and decomposition products alongside Mg deposition and ligand exchange. | [80] |
| Retained surface benefit Mg(pftb)₂ + MgCl₂ / THF | 99.7 | Mg charge recovery over a 3000-cycle readout | Replace the liquid; verify film persistence and retained Mg transfer. | [20] |
| Coupled liquid and film effects Mg(OTf)₂ + MgCl₂ / DME–TEP | 99.4 | Mg∥Mo charge recovery after 3000 h | Vary the liquid and conditioned surface independently; resolve their contributions. | [88] |
| Compatibility at both electrodes Mg(OTf)₂ / G2–MOEA | 98.3 | Average Mg CE after 8200 cycles in an asymmetric cell | Retest Mg reversibility after cathode exposure; isolate each electrode response. | [87] |

CE is the common source-reported Mg plating/stripping endpoint. Cycling windows retain each source’s context; protocols are not normalised and the values are not a performance ranking. The matched tests are proposed controls. High CE alone does not establish faster release, anion regeneration or the absence of kinetic trapping. “Via” identifies Zhang et al. [86] as the numerical source; the other values were checked in original abstracts.

Chemistries identify representative systems, not complete recipes. DME: 1,2-dimethoxyethane; G2: diglyme; BTFE: bis(2,2,2-trifluoroethyl) ether; THF: tetrahydrofuran; TEP: triethyl phosphate; MOPA-1: 1-methoxy-2-propylamine; MOEA: 2-methoxyethylamine; pftb: perfluorinated tert-butoxide; OTf: triflate; TFSI: bis(trifluoromethanesulfonyl)imide. Reference numbers retain the V7 manuscript order and link to DOI records.