# Table 1. Representative electrolyte strategies reveal multiple kinetic pathways for magnesium transfer.

| Design strategy | Representative chemistry | Reported Mg CE (%) | Reported readout context | Mechanistic question to test | Source refs. |
| --- | --- | --- | --- | --- | --- |
| Weakly coordinating anion | Mg(CB₁₁H₁₂)₂/G4 | >94.4 | Mg reversibility; value compiled by Zhang et al. | Does solvent rearrangement remain accessible as persistent anion association is reduced? | [44] via [86] |
| Weakly coordinating anion | Mg perfluorinated pinacolatoborate (Mg-FPB) | 95 | Original report of reversible Mg deposition | Does weak anion association leave solvent rearrangement as the main limitation? | [48] |
| Promote pair dissociation | Mg(TFSI)₂/DME–G2–BTFE–TEP | 95.2 | Mg plating/stripping; value compiled by Zhang et al. | Does dissociation increase reactive precursor availability independently of surface and growth changes? | [24] via [86] |
| Introduce primary-shell pairing | Weakly solvated amine + strongly coordinating Mg salt | 99.6 | CE reported for 800 cycles | Pairing suppresses amine reduction and H₂ evolution; does ligand exchange also change? | [80] |
| Reshape solvent coordination | Mg(TFSI)₂/DME–MOPA-1 | 99.5 | Mg plating/stripping; value compiled by Zhang et al. | Does modified solvent coordination speed rearrangement, charge transfer or both? | [76] via [86] |
| Mixed-ion coordination | Mg(TFSI)₂ + LiOTf/DME–TMP | 98 | Original report of Mg-metal reversibility | How much comes from altered Mg–DME interaction versus the phosphate-rich interface? | [83] |
| Coordinate salt and solvent | Mg(OTf)₂/G2–MOEA | 98.3 | Asymmetric-cell average CE after 8200 cycles; symmetric lifetime reported separately | How do coordination and distinct electrode interphases share the contribution to reversibility? | [87] |
| Chloride complexes + interphase | Mg(pftb)₂ + MgCl₂/THF | 99.7 | CE reported over 3000 cycles; symmetric lifetime is separate | Does a retained hybrid interphase sustain transfer when solution coordination is changed? | [20] |
| Dissociation + interphase | Mg(OTf)₂ + MgCl₂/DME–TEP | 99.4 | Mg¦¦Mo: 0.5 mA cm⁻², 0.25 mAh cm⁻²; CE reported after 3000 h | Can a molecular transfer gain be separated from suppressed losses at the interphase? | [88] |
| Mixed donors + chloride carrier | Mg(OTf)₂ + MgCl₂/DME–MOEA | >92.3 | Reported Mg CE; donor ratio MOEA:DME = 1:6 (v/v) | Does the gain follow the modified carrier, the surface layer or both when cathode chemistry changes? | [89] |

CE is the shared reported endpoint, not a rate or barrier measurement. Independent protocols and unspecified averaging windows prevent a performance ranking. The readout retains each source's reported context; symmetric lifetime and full-cell efficiency are excluded. Cross-system kinetics require matched current, capacity, substrate, temperature and conditioning.

The chemistry identifies the design, not a complete recipe. Mechanistic questions are proposed tests. For the carborane, solvent-designed TFSI and MOPA-1 rows, “via” identifies Zhang et al. [86] as the accessed numerical source; the original study identifies the chemistry. The other values were checked in original abstracts. Protocol and source-access limits are recorded separately. Reference numbers link to DOI records.

THF: tetrahydrofuran; DME: 1,2-dimethoxyethane; G2/G4: diglyme/tetraglyme; BTFE: bis(2,2,2-trifluoroethyl) ether; TMP/TEP: trimethyl/triethyl phosphate; MOPA-1: 1-methoxy-2-propylamine; MOEA: 2-methoxyethylamine; pftb: perfluorinated tert-butoxide; OTf: triflate; TFSI: bis(trifluoromethanesulfonyl)imide. TMP denotes the phosphate here, not the piperidide ligand used in some Hauser bases.