Table 2. Perturbations and outcomes that distinguish contributions to magnesium transfer

| Possible contribution | Matched perturbation | Observation favouring or limiting the explanation | Studies motivating the test |
| --- | --- | --- | --- |
| Precursor availability | Vary association at matched transport and surface conditions. | Raman/NMR: carrier population tracks Mg current at unchanged exchange; transport or film changes confound attribution. | [24,82] |
| Ligand departure or rearrangement | Vary donor/anion identity on equally conditioned surfaces. | Exchange NMR or validated MD: exchange tracks Mg current; faster exchange without a current gain suggests a later bottleneck. | [25,39,76] |
| Suppression of unwanted reduction | Measure Mg current, gas and soluble/film products. | Less H₂ or decomposition at matched Mg deposition and exchange supports selectivity; shell structure alone is insufficient. | [31,80] |
| Repeated molecular assistance | Track active anion and products against Mg throughput. | Active-species recovery plus repeated kinetic benefit supports reuse; survival alone does not establish turnover. | [20,81] |
| Persistent intermediate | Resolve residence time and the escape free-energy barrier. | Long residence plus a high local escape barrier supports trapping; low cluster energy alone does not. | [23,32] |
| Retained surface benefit | Replace liquid; verify film persistence and impedance. | Retained activity with an intact film supports a surface contribution; film dissolution makes activity loss inconclusive. | [20,88] |
| Coupled molecular and film effects | Separate initial liquid and retained-surface responses; quantify products. | Interacting liquid and film responses support coupling; CE alone cannot apportion their contributions. | [88,90] |

Solvation shapes the starting states; its effect on magnesium transfer depends on the reaction pathways they can access.

Contributions can overlap. References motivate the tests; they do not establish every listed measurement or anion regeneration. Exchange measurements require suitable time resolution. The outer-shell example uses a neutral additive.