# Table 1. Representative magnesium plating and stripping properties across electrolyte strategies.

| Electrolyte composition | j (mA cm⁻²) | Q (mAh cm⁻²) | Eplate (V) | η (V) | CE (%) | Cycle lifespan | Distinctive feature | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Mg–Al chloride electrolyte/THF | N.V. | N.V. | N.V. | N.V. | 100 (first cycle) | N.V. | Chloride participation; conditioning-free Mg transfer | [63] P |
| Mg–Li chloride complex + BTFE (MLCC) | 5 | N.V. | N.V. | N.V. | N.V. | 1200 h (Mg¦¦Mg) | Charged chloride clusters; reversible cycling also at 20 mA cm⁻² | [81] P |
| Mg(pftb)₂ + MgCl₂/THF | N.V. | N.V. | N.V. | N.V. | 99.7 | 3000 cycles (CE test) | Chloride coordination and an organic/inorganic SEI | [20] P |
| Mg salt/weakly solvated amineᵃ | N.V. | N.V. | N.V. | N.V. | 99.6 | 800 cycles (CE test) | Primary-shell ion pairing suppresses amine reduction and H₂ evolution | [79] P |
| 0.18 M Mg(TFSI)₂ + 0.1 M LiOTf/DME–TMP | N.V. | N.V. | −0.22 | N.V. | 98 | 450 hᵇ | Mixed solvation and a phosphate-rich interphase | [82] P/S |
| Screened amine electrolyteᵃ | 1 | N.V. | N.V. | 0.060 | N.V. | N.V. | Counterpoised solvent–anion interactions; MgH₂-containing interphase | [24] P |
| MgEDTF/DME; MgEDTF + trace halide/DME | N.V. | N.V. | N.V. | 0.24; <0.20ᶜ | N.V. | N.V. | EDTF²⁻ chelation; non-chelating control has η = 2.0 V | [80] P |
| Mg(CB₁₁H₁₂)₂/G4 | N.V. | N.V. | N.V. | N.V. | >94.4 | N.V. | Weakly coordinating carborane; chloride-free design | [43] S |
| Mg-FPB electrolyteᵃ | N.V. | N.V. | N.V. | 0.197 | 95 | N.V. | Weakly coordinating fluorinated pinacolatoborate | [47] P |
| 0.4 M Mg(TFSI)₂/DME–G2–BTFE–TEP | N.V. | 2ᵇ | −0.15 | N.V. | 95.2 | 7000 hᵇ | Weak ion pairing; ion-pair dissociation promoted | [23] P/S |
| Mg[B(hfip)₄]₂/DME–THF (DME:THF = 1:1, v/v) | 10ᵇ | N.V. | N.V. | 0.120 | N.V. | >1200 hᵇ | Competitive ether coordination; control has η = 0.316 V at 8 mA cm⁻² | [51] P |
| 0.5 M Mg(TFSI)₂/DME–MOPA-1 | N.V. | N.V. | ≈−0.10 | N.V. | 99.5 | ≈190 hᵇ | Amine-assisted solvation-shell reorganization | [75] S |
| 0.25 M Mg(OTf)₂/G2–MOEA | N.V. | N.V. | −0.13 to −0.26 | N.V. | 98.3 (average) | 8200 cycles (CE); >5000 h (Mg¦¦Mg)ᵇ | Mixed coordination and electrode-specific interphases | [83] P/S |
| 0.3 M EtMgCl/MOB (1:2 molar ratio) | 5 | N.V. | N.V. | N.V. | N.V. | >1000 cycles (Mg¦¦Mo) | Dipole interactions and an organic/inorganic interphase | [84] P |
| Mg(OTf)₂ + MgCl₂/DME–TEP | 0.5 | 0.25 | N.V. | N.V. | 99.4 | 3000 h (Mg¦¦Mo) | Salt dissociation and interphase regulation | [85] P |
| [Mg(THF)₆][AlCl₄]₂ + LiCl/THF | 0.5 | N.V. | N.V. | 0.140/0.140ᵈ | N.V. | N.V. | LiCl dissolves blocking MgCl₂ and exposes fresh Mg | [86] P |

j, current density; Q, areal capacity; Eplate, reported plating potential; η, reported overpotential; CE, Coulombic efficiency. N.V., value not verified in the accessed source. P, original-paper abstract; S, supplied AM Perspective (DOI 10.1002/adma.202417652); P/S, combined sources.

ᵃ Complete formulation or solvent identity unverified. ᵇ Values may describe separate tests; j and Q are not automatically the conditions of the CE/lifetime test. In [51], j = 10 applies to η = 0.120 V; cycling j is N.V. In [83], CE and Mg||Mg lifetime are separate tests. ᶜ With trace Cl⁻/Br⁻. ᵈ Plating/stripping, respectively. Eplate reference conventions remain unverified. Reference numbers follow Perspective V3 and link to the original DOI.

Abbreviations: THF, tetrahydrofuran; DME, 1,2-dimethoxyethane; G2/G4, diglyme/tetraglyme; BTFE, bis(2,2,2-trifluoroethyl) ether; TMP/TEP, trimethyl/triethyl phosphate; MOPA-1, 1-methoxy-2-propylamine; MOEA, 2-methoxyethylamine; MOB, 1,4-oxazinane borane; Mg-FPB, magnesium perfluorinated pinacolatoborate; MgEDTF, magnesium salt of the chelating dianion EDTF²⁻; pftb, perfluorinated tert-butoxide; hfip, hexafluoroisopropoxide.