# Table 1. Representative electrolyte strategies reveal multiple kinetic pathways for magnesium transfer.

| Design strategy | Representative chemistry | Mg CE (%) | Mechanistic question raised by the result | Ref. |
| --- | --- | --- | --- | --- |
| Weakly coordinating anion | Mg(CB₁₁H₁₂)₂/G4 | >94.4 | Does solvent rearrangement remain accessible as persistent anion association is reduced? | [43]⁠S |
| Weakly coordinating anion | Mg perfluorinated pinacolatoborate (Mg-FPB) | 95 | Does weak anion association leave solvent rearrangement as the main limitation? | [47]⁠P |
| Promote pair dissociation | Mg(TFSI)₂/DME–G2–BTFE–TEP | 95.2 | Does dissociation increase reactive precursor availability, independently of surface and growth changes? | [23]⁠S |
| Introduce primary-shell pairing | Weakly solvated amine + strongly coordinating Mg salt | 99.6 | Pairing suppresses amine reduction and H₂ evolution; does ligand exchange also change? | [79]⁠P |
| Reshape solvent coordination | Mg(TFSI)₂/DME–MOPA-1 | 99.5 | Does modified solvent coordination speed ligand rearrangement, charge transfer, or both? | [75]⁠S |
| Mixed-ion coordination | Mg(TFSI)₂ + LiOTf/DME–TMP | 98 | How much of the benefit comes from altered Mg–DME binding versus the phosphate-rich interface? | [82]⁠P |
| Coordinate both salt and solvent | Mg(OTf)₂/G2–MOEA | 98.3 | How do coordination and distinct electrode interphases share the contribution to reversibility? | [85]⁠P/S |
| Chloride complexes + interphase | Mg(pftb)₂ + MgCl₂/THF | 99.7 | Does a retained hybrid interphase sustain transfer after the original solution is replaced? | [20]⁠P |
| Dissociation + interphase | Mg(OTf)₂ + MgCl₂/DME–TEP | 99.4 | Can faster molecular transfer be separated from suppression of losses by the interphase? | [86]⁠P |

Selection: every entry reports Mg plating/stripping Coulombic efficiency (CE), the shared quantitative endpoint. First-cycle-only CE, symmetric-cell lifetimes and full-cell efficiencies are excluded from this column. Values retain the reported precision; 98.3% is a reported average. These are independent protocols, not a common-condition ranking or measurements of a desolvation barrier.

The chemistry column identifies the reported design, not a complete recipe. Mechanistic questions are proposed tests, not established rate-limiting steps. P: original-paper abstract supports the CE; S: supplied AM Perspective [87], pp. 4–5 (DOI 10.1002/adma.202417652); P/S: primary CE and secondary formulation. Current, capacity, substrate, conditioning and averaging windows should be matched in future comparisons; accessed-source limits are recorded in the companion audit. Reference numbers link to DOI records.

THF: tetrahydrofuran; DME: 1,2-dimethoxyethane; G2/G4: diglyme/tetraglyme; BTFE: bis(2,2,2-trifluoroethyl) ether; TMP/TEP: trimethyl/triethyl phosphate; MOPA-1: 1-methoxy-2-propylamine; MOEA: 2-methoxyethylamine; pftb: perfluorinated tert-butoxide; OTf: triflate; TFSI: bis(trifluoromethanesulfonyl)imide.