# Table 1. Representative electrolyte strategies reveal multiple kinetic pathways for magnesium transfer.

| Electrolyte composition | j (mA cm⁻²) | Q (mAh cm⁻²) | Eplate (V) | η (V) | CE (%) | Cycle lifespan | Pathway suggested | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Mg–Al chloride electrolyte/THF | N.V. | N.V. | N.V. | N.V. | 100 (first cycle) | N.V. | D Surface activation without prolonged conditioning | [63]⁠P |
| Mg–Li chloride complex + BTFE (MLCC) | 5 | N.V. | N.V. | N.V. | N.V. | 1200 h (Mg¦¦Mg) | A/D Charged carriers and interphase formation | [81]⁠P |
| Mg(pftb)₂ + MgCl₂/THF | N.V. | N.V. | N.V. | N.V. | 99.7 | 3000 cycles (CE test) | D Transfer sustained by an organic/inorganic interphase | [20]⁠P |
| Mg salt/weakly solvated amineᵃ | N.V. | N.V. | N.V. | N.V. | 99.6 | 800 cycles (CE test) | C Pairing limits amine reduction and H₂ evolution | [79]⁠P |
| 0.18 M Mg(TFSI)₂ + 0.1 M LiOTf/DME–TMP | N.V. | N.V. | −0.22 | N.V. | 98 | 450 hᵇ | B/D Modified coordination and phosphate-rich interphase | [82]⁠P/S |
| Screened amine electrolyteᵃ | 1 | N.V. | N.V. | 0.060 | N.V. | N.V. | B/D Proposed synchronous release and MgH₂ interphase | [24]⁠P |
| MgEDTF/DME; MgEDTF + trace halide/DME | N.V. | N.V. | N.V. | 0.24; <0.20ᶜ | N.V. | N.V. | B/D Chelating-anion pathway and SEI (control η = 2.0 V) | [80]⁠P |
| Mg(CB₁₁H₁₂)₂/G4 | N.V. | N.V. | N.V. | N.V. | >94.4 | N.V. | A Weak coordination through carborane design | [43]⁠S |
| Mg-FPB electrolyteᵃ | N.V. | N.V. | N.V. | 0.197 | 95 | N.V. | A Weak coordination through pinacolatoborate design | [47]⁠P |
| 0.4 M Mg(TFSI)₂/DME–G2–BTFE–TEP | N.V. | 2ᵇ | −0.15 | N.V. | 95.2 | 7000 hᵇ | A Ion-pair dissociation | [23]⁠P/S |
| Mg[B(hfip)₄]₂/DME–THF (DME:THF = 1:1, v/v) | 10ᵇ | N.V. | N.V. | 0.120 | N.V. | >1200 hᵇ | B Competitive ether release (control: 0.316 V at 8 mA cm⁻²) | [51]⁠P |
| 0.5 M Mg(TFSI)₂/DME–MOPA-1 | N.V. | N.V. | ≈−0.10 | N.V. | 99.5 | ≈190 hᵇ | B Solvent-shell rearrangement | [75]⁠S |
| 0.25 M Mg(OTf)₂/G2–MOEA | N.V. | N.V. | −0.13 to −0.26 | N.V. | 98.3 (average) | 8200 cycles (CE); >5000 h (Mg¦¦Mg)ᵇ | B/D Mixed coordination and distinct electrode interphases | [85]⁠P/S |
| 0.3 M EtMgCl/MOB (1:2 molar ratio) | 5 | N.V. | N.V. | N.V. | N.V. | >1000 cycles (Mg¦¦Mo) | B/D Dipole-regulated release and organic/inorganic film | [86]⁠P |
| Mg(OTf)₂ + MgCl₂/DME–TEP | 0.5 | 0.25 | N.V. | N.V. | 99.4 | 3000 h (Mg¦¦Mo) | A/D Dissociation and stable interphase | [87]⁠P |
| [Mg(THF)₆][AlCl₄]₂ + LiCl/THF | 0.5 | N.V. | N.V. | 0.140/0.140ᵈ | N.V. | N.V. | D Removal of blocking MgCl₂ | [88]⁠P |

Pathways: A, avoid persistent association; B, change ligand release or rearrangement; C, suppress side reactions; D, activate the surface or sustain transfer through an interphase. These overlapping assignments are interpretations to test, not proof of the rate-limiting step. P/S labels verify numerical sources, not every pathway assignment.

j, current density; Q, areal capacity; Eplate, reported plating potential; η, reported overpotential; CE, Coulombic efficiency. N.V., value not verified in the accessed source. P, original-paper abstract; S, supplied AM Perspective [89] (DOI 10.1002/adma.202417652); P/S, combined sources.

ᵃ Complete formulation or solvent identity unverified. ᵇ Values may describe separate tests; j and Q are not automatically the CE/lifetime conditions. In [51], j = 10 applies to η = 0.120 V; cycling j is N.V. In [85], CE and Mg||Mg lifetime are separate tests. Reversible cycling at 20 mA cm⁻² is also reported in [81]. ᶜ With trace Cl⁻/Br⁻. ᵈ Plating/stripping, respectively. Eplate reference conventions remain unverified. Each reference number links to its DOI.

Abbreviations: THF, tetrahydrofuran; DME, 1,2-dimethoxyethane; G2/G4, diglyme/tetraglyme; BTFE, bis(2,2,2-trifluoroethyl) ether; TMP/TEP, trimethyl/triethyl phosphate; MOPA-1, 1-methoxy-2-propylamine; MOEA, 2-methoxyethylamine; MOB, 1,4-oxazinane borane; Mg-FPB, magnesium perfluorinated pinacolatoborate; MgEDTF, magnesium salt of EDTF²⁻; pftb, perfluorinated tert-butoxide; hfip, hexafluoroisopropoxide.